| plyboostrand®, Neopolitan™ Bamboo plywood product specification in CSi 3-part format | Smith & Fong Company 475 - 6th Street San Francisco, CA 94103 Phone: (415) 896-0577 Toll Free: (866) 835-9859 Fax: (415) 896-0583 Website: www.plyboo.com E-mail: sales@plyboo.com |
| --- | --- |

******************************************************************************

GENERAL NOTES TO SPECIFIER: pLEASE GO TO WWW.PLYBOO.COM AND CHECK IN THE SPECIFICATIONS SECTION TO VERIFY THIS IS THE MOST CURRENT VERSION. THE FOLLOWING PRODUCT SPECIFICATION LANGUAGE IS INTENDED TO ASSIST DESIGN PROFESSIONALS IN specifying bamboo plywood in EXISTING 3-part specifications for paneling, casework, doors, and similar architectural woodwork. SAMPLE LANGUAGE IS PROVIDED FOR APPLICABLE ARTICLES IN PART 1–GENERAL AND PART 2–PRODUCTS FOLLOWING THE CONSTRUCTION SPECIFICATION INSTITUTE’S SECTIONFORMAT. BECAUSE OF THE VARIATION IN SPECIFICATION SYSTEMS CURRENTLY IN USE, ARTICLE AND PARAGRAPH numbers and TITLES MAY DIFFER SOMEWHAT THAN PRESENTED HEREIN. THE SAMPLE LANGUAGE SHOULD BE EDITED ACCORDINGLY TO FIT EACH FIRM’S SPECIFICATIONS. ARTICLES AND PARAGRAPHS OF THIS PRODUCT SPECIFICATION ASSUME THE PROJECT MANUAL WILL CONTAIN COMPLETE DIVISION 1 DOCUMENTS INCLUDING 01 25 13(PRODUCT SUBSTITUTION PROCEDURES, SECTIONS 01 33 00(SUBMITTAL PROCEDURES, 01 62 00(PRODUCT OPTIONS, 01 66 00(PRODUCT STORAGE AND HANDLING REQUIREMENTS, 01 74 00(cLEANING and waste management, 01 77 00(CLOSEOUT PROCEDURES, AND 01 78 00(CLOSEOUT SUBMITTALS. CLOSE COORDINATION WITH DIVISION 1 SECTIONS IS REQUIRED. IF THE PROJECT MANUAL DOES NOT CONTAIN THESE SECTIONS, ADDITIONAL INFORMATION MAY BE INCLUDED UNDER THE APPROPRIATE ARTICLES. NOTES TO THE SPECIFIER ARE IN ALL UPPER CASE TEXT AND ARE CONTAINED within rows of asterisks. GREY HIGHLIGHTED GREEN TEXT AND NOTES RELATE TO LEED® PROJECTS AND CAN BE DELETED IF THE PROJECT IS NOT INTENDED TO ATTAIN leed CERTIFICATION. OPTIONAL ITEMS REQUIRING SELECTION BY THE SPECIFIER ARE ENCLOSED WITHIN BRACKETS, E.G. [35] [40] [45]. MAKE APPROPRIATE SELECTIONS AND DELETE OTHERS.

******************************************************************************

# PART 1–GENERAL

  - SUMMARY

### Section Includes:

*************************************************************************************

ADD SUBPARAGRAPH IDENTIFYING THE ITEMS MADE WITH BAMBOO PLYWOOD.

### ******************************************************************************

### Related Sections:

*************************************************************************************

INCLUDE ALL DIVISION 01 SECTIONS  CONTAINING LEED® REQUIREMENTS.

INCLUDE SECTION 01350 IF THE PROJECT IS A SCHOOL LOCATED IN A DISTRICT USING “SECTION 01350 – SPECIAL ENVIRONMENTAL REQUIREMENTS” http://www.chps.net/manual/index.htm#specs PREPARED BY THE COLLABORATIVE FOR HIGH PERFORMANCE SCHOOLS (CHPS).

*************************************************************************************

1.02	REFERENCES

*************************************************************************************

IF THE “REFERENCES” ARTICLE IS USED, INCLUDE THE FOLLOWING IN THE REFERENCE LIST:

*************************************************************************************

### A.	ASTM - American Society for Testing and Materials:

#### 1.  ASTM D 1037, Standard Test Methods for Evaluating Properties of Wood-

#### Base Fiber and Particle Panel Materials.

#### 2.  ASTM D 3043 Standard Test Methods for Flexural Structural Panels in

#### Flexure.

#### 3.  ASTM E 84, Standard Test Method for Surface Burning Characteristics of

#### Building Materials.

#### 4.  ASTM D 4442, Standard Test Methods for Direct Moisture Content

#### Measurement of Wood and Wood-Base Materials.

#### 5.  ASTM D 3500, Standard Test Method for Structural Panels in Tension.

### B.    American National Standards Institute/Hardwood Plywood and Veneer Association

### C.     US Green Building Council’s Leadership in Energy and Environmental Design Green Building Rating System™ (LEED).

1.03	SUBMITTALS

A. 	Product Data:

*************************************************************************************

INCLUDE THE FOLLOWING IN THE “PRODUCT DATA” PARAGRAPH:

*************************************************************************************

1.	Bamboo plywood manufacturer’s product data.

B.	LEED Submittals:

*************************************************************************************

INCLUDE THE FOLLOWING FOR LEED PROJECTS, AS APPLICABLE.

*************************************************************************************

#### Credit MR 6, Rapidly Renewable Materials: Bamboo manufacturer’s product data for each product used, indicating that product(s) are manufactured from a rapidly renewable resource.

#### Credit EQ 4.4, Low Emitting Materials: Composite Wood & Agrifiber Products: Manufacturer’s product data.

1.04	WARRANTY

*************************************************************************************

INCLUDE THE FOLLOWING WARRANTY

*************************************************************************************

A. 	A Warranty for Smith & Fong Plyboo Products referenced at www.plyboo.com

PART 2–PRODUCTS

2.01	MATERIALS

*************************************************************************************

INCLUDE THE FOLLOWING PARAGRAPHS AND SUBPARAGRAPHS FOR BAMBOO PLYWOOD AS APPROPRIATE.

*************************************************************************************

A.	Bamboo Plywood:

- Manufacturer: Smith & Fong Company, San Francisco, CA 94103

##### Tel: (866) 835-9859.

##### http://www.plyboo.com/

- Species: Moso (Phyllostachys Pubescens)

- Manufactured without added urea formaldehyde.

*************************************************************************************

INCLUDE THE FOLLOWING SUBPARAGRAPH IF PRODUCTS ARE USED FOR WALL OR CEILING FINISHES PURSUANT TO IBC SECTION 803.

*************************************************************************************

- Fire Resistance Classification: [Class C].

##### Test surface burning characteristics in accordance with ASTM E 84.

*************************************************************************************

SELECT APPROPRIATE TYPE(S) BELOW TO SUIT PROJECT REQUIREMENTS. DELETE THOSE NOT USED. FABRICATION ARTICLE OR DRAWINGS MUST CLEARLY IDENTIFY SPECIFIC USES.

PRODUCTS:   GO TO http://www.plyboo.com/ FOR AVAILABLE FACE DIMENSIONS.

5. Type

##### a.     3/4 inch thick, 3-ply

##### i. [Neopolitan] [Sahara Strand] [Havana Strand]

##### ii. No added Urea Formaldehyde

##### b.     5/32 inch thick (4 mm), 1-ply

##### i. [Neopolitan] [Sahara Strand] [Havana Strand]

##### ii. No added Urea Formaldehyde

6. Physical/Mechanical Properties:

              - ASTM D 3043 Method D Flexural Strength (MOE/MOR)

¾ inch thick, 3-ply, Cross Core Strand:  268 MOE/14,760 MOR

              - ASTM D 1037 Screw Hold

¾ inch thick, 3-ply, Cross Core Strand

- Face: 742 pounds

- Back: 831 pounds

- Edge 1: 980 pounds

- Edge 2: 759 pounds

              - ASTM D 4442 Method A Moisture Content

¾ inch thick, 3-ply, Cross Core Strand: average 6 - 9 percent

              - ASTM D 1037 Tensile Strength Parallel

¾ inch thick, 3-ply, Cross Core Strand:  Load 1732 pounds,

Strength 5968 psi

              - ASTM D 3500 Tensile Strength Perpendicular

¾ inch thick, 3-ply, Cross Core Strand: Load 1591 pounds, Strength 1061 psi

              - ASTM D 1037 Dimensional Stability: at 20% RH

¾ inch thick, 3-ply, Cross Core Strand

- Linear Expansion: Parallel –0.04 percent; Perpendicular –0.07 percent

- Thickness Swell: -0.13 percent

              - ASTM E 84 Surface Burning

¾ inch thick Cross Core Strand: Class C

B.   Accessories

a.   Edge Banding, 7/8 inch width by 1/16 inch (2mm) thickness by 72

inch length

i.  [Neopolitan] [Sahara Strand] [Havana Strand]

ii.  No added Urea Formaldehyde

End OF PRODUCT SPECIFICATION